SECTION 07 22 00

ROOF INSULATION

NOTE:  This guide specification is provided as a guideline and must be modified, as required, by the Designer of Record for each project. This specification is prepared in general accordance with CSI format to be included under Division 7 – Thermal and Moisture Protection.  Additional information is provided.  [delete this paragraph]

Optional information is presented in “blue” font below.  Choose appropriate options, delete as necessary.  [delete this paragraph]

- GENERAL

  - SUMMARY

    - Work shall include, but is not limited to, the following:

      - Preparation of existing (new) roof deck and all flashing substrates.

      - Thermal Barrier

      - Insulation

      - Cover-board

      - All related materials and labor required to complete specified roofing necessary to receive specified manufacturer’s warranty.

  - RELATED SECTIONS

    - Division 010000 – General Requirements

    - Division 011000 – Summary of Work

    - Division 071416 – Cold Fluid-Applied Waterproofing

    - Division 072713 – Modified Bituminous Sheet Vapor Retarders

    - Division 075213 – Atactic Polypropylene (APP) Modified Bitumen Membrane Roofing

    - Division 075216 – Styrene-Butadiene-Styrene (SBS) Modified Bitumen Membrane Roofing

    - Division 076200 – Sheet Metal Flashing and Trim

  - DEFINITIONS

    - ASTM D 1079-Definitions of Term Relating to Roofing and Waterproofing.

    - The National Roofing Contractors Association (NRCA) Roofing and Waterproofing Manual, Fifth Edition Glossary.

  - REFERENCES

    - AMERICAN SOCIETY OF CIVIL ENGINEERS - Reference Document ASCE 7, Minimum Design Loads for Buildings and Other Structures.

    - AMERICAN STANDARD OF TESTING METHODS (ASTM):

      - ASTM C 726 - Standard Specification for Mineral Wool Roof Insulation Board.

      - ASTM C 728 - Standard Specification for Perlite Thermal Insulation Board.

      - ASTM C 1177/C 1177M - Standard Specification for Glass Mat Gypsum Substrate for Use as Sheathing.

      - ASTM C 1278 - Standard Specification for Fiber-Reinforced Gypsum Panel.

      - ASTM C 1289 - Standard Specification for Faced Rigid Cellular Polyisocyanurate Insulation Board.

      - ASTM C 1325 – Standard Specification for Non-Asbestos Fiber-Mat Reinforced Cementitious Backer Units.

      - ASTM D 41 - Standard Specification for Asphalt Primer Used in Roofing, Damp proofing, and Waterproofing.

    - AMERICAN NATIONAL STANDARDS INSTITUTE (ANSI)::

      - ANSI/SPRI FX-1, Standard Field Test Procedure for Determining the Withdrawal Resistance of Roofing Fasteners.

      - ANSI/SPRI IA-1, Standard Field Test Procedure for Determining the Mechanical Uplift Resistance of Insulation Adhesives over Various Substrates.

      - ANSI/FM 4474- American National Standard for Evaluating the Simulated Wind Resistance of Roof Assemblies Using Static Positive and/or Negative Differential Pressures.

    - CANADIAN GENERAL STANDARDS BOARD (CGSB):

      - CGSB 37-GP 56M- Standard for: Modified Bituminous, Prefabricated, and Reinforced for Roofing.

    - FACTORY MUTUAL (FM):

      - FM 4450 - Approval Standard - Class I Insulated Steel Roof Decks.

      - FM 4470 - Approval Standard - Class I Roof Covers.

    - FLORIDA BUILDING CODE (FBC):

      - 20XX Florida Building Code (FBC).

    - INTERNATIONAL CODES COUNCIL (ICC):

      - 20XX International Building Code (IBC).

    - NATIONAL ROOFING CONTRACTORS ASSOCIATION (NRCA).

    - UNDERWRITERS LABORATORY (UL):

      - UL 790 Standard Test Methods for Fire Tests of Roof Coverings.

      - UL 1256 – Fire Test of Roof Deck Constructions.

  - ACTION SUBMITTALS

    - Product Data Sheets: Submit manufacturer’s product data sheets, installation instructions and/or general requirements for each component.

    - Safety Data Sheets: Submit manufacturer’s Safety Data Sheets (SDS) for each component.

    - Sample/Specimen Warranty from the manufacturer and contractor.

    - Shop Drawings: Provide roof plan and applicable roof system detail drawings.

  - INFORMATIONAL SUBMITTALS

    - Contractor Certification: Submit written certification from roofing system manufacturer certifying that the applicator is authorized by the manufacturer to install the specified materials and system.

  - CLOSEOUT SUBMITTALS

    - Warranty: Provide manufacturer’s and contractor’s warranties upon substantial completion of the roofing system.

  - QUALITY ASSURANCE

    - MANUFACTURER QUALIFICATIONS:

      - Manufacture shall have 20 years of experience manufacturing roofing materials.

      - Trained Technical Field Representatives, employed by the manufacturer, independent of sales.

      - Provide reports in a timely manner of all site visit reports.

      - Provide specified warranty upon satisfactory project completion.

    - CONTRACTOR QUALIFICATIONS:

      - Contractor shall be authorized by the manufacturer to install specified materials prior to the bidding period through satisfactory project completion.

      - Applicators shall have completed projects of similar scope using same materials as specified herein.

      - Contractor shall provide full time, on-site superintendent or foreman experienced with the specified roof system through satisfactory project completion.

      - Applicators shall be skilled in the application methods for all materials.

      - Contractor shall maintain a daily record, on-site, documenting material installation and related project conditions.

      - Contractor shall maintain a copy of all submittal documents, on-site, available at all times for reference.

  - DELIVERY, STORAGE AND HANDLING

    - Refer to each product data sheet or other published literature for specific requirements.

    - Deliver materials and store them in their unopened, original packaging, bearing the manufacturer's name, related standards, and any other specification or reference accepted as standard.

    - Protect and store materials in a dry, well-vented, and weatherproof location. Only materials to be used the same day shall be removed from this location.

    - When materials are to be stored outdoors, store away from standing water, stacked on raised pallets or dunnage, at least 4 in or more above ground level.  Carefully cover storage with “breathable” tarpaulins to protect materials from precipitation and to prevent exposure to condensation.

    - Properly dispose of all product wrappers, pallets, cardboard tubes, scrap, waste, and debris.  All damaged materials shall be removed from job site and replaced with new, suitable materials.

  - SITE CONDITIONS

    - SAFETY:

      - The contractor shall be responsible for complying with all project-related safety and environmental requirements.

      - Refer to NRCA CERTA recommendations, local codes and building owner’s requirements for hot work operations.

      - The contractor shall review project conditions and determine when and where conditions are appropriate to utilize the specified liquid-applied, or semi-solid roofing materials.  When conditions are determined by the contractor to be unsafe or undesirable to proceed, measures shall be taken to prevent or eliminate the unsafe or undesirable exposures and conditions, or equivalent approved materials and methods shall be utilized to accommodate requirements and conditions.

      - The contractor shall review project conditions and determine when and where conditions are appropriate to utilize the specified hot asphalt-applied materials.  When conditions are determined by the contractor to be unsafe or undesirable to proceed, measures shall be taken to prevent or eliminate the unsafe or undesirable exposures and conditions, or equivalent approved materials and methods shall be utilized to accommodate requirements and conditions. .

      - The contractor shall refer to product Safety Data Sheets (SDS) for health, safety, and environment related hazards, and take all necessary measures and precautions to comply with exposure requirements.

    - ENVIRONMENTAL CONDITIONS:

      - Monitor substrate temperature and material temperature, as well as all environmental conditions such as ambient temperature, moisture, sun, cloud cover, wind, humidity, and shade.  Ensure conditions are satisfactory to begin work and ensure conditions remain satisfactory during the installation of specified materials.  Materials and methods shall be adjusted as necessary to accommodate varying project conditions.  Materials shall not be installed when conditions are unacceptable to achieve the specified results.

      - Precipitation and dew point:  Monitor weather to ensure the project environment is dry before, and will remain dry, during the application of roofing materials.   Ensure all roofing materials and substrates remain above the dew point temperature as required to prevent condensation and maintain dry conditions.

      - Mopping asphalt application:  Primer, where used, shall be fully dry before applying hot asphalt.  Take all necessary measures and monitor all conditions, to ensure the specified asphalt temperature is no less than 400(F (204(C) at the point of contact with the specified membrane as it is rolled into the hot asphalt.

  - PERFORMANCE REQUIREMENTS

    - FIRE CLASSIFICATION:

      - Roof construction performance testing shall be in accordance with UL 1256, FM 4450 or FM 4470 to meet the specified requirements for interior flame spread and fuel contribution.

        - Roof construction meets requirements of UL 1256, or FM Class 1.

    - ROOF SLOPE:

      - Finished roof slope shall be ¼ inch per foot (2 percent) minimum for roof drainage.

    - ENERGY CONSERVATION REQUIREMENTS:

      - Polyisocyanurate Insulation "R" Value:  Long-term thermal resistance (LTTR) values of the specified foam insulation shall be determined in accordance with CAN/ULC-S770.

      - Polyisocyanurate Insulation "R" Value:  Shall be determined in accordance with ASTM C1289-11a.

      - Thermal Resistance ‘R’ for the specified roof insulation system shall include the continuous insulation (ci) above the roof deck.

        - Total Thermal Resistance R Value, continuous insulation (ci) above-deck: R(00)

- PRODUCTS

  - MANUFACTURER

    - SINGLE SOURCE MANUFACTURER: All roofing materials shall be provided by a single supplier with 20 years or more manufacturing history in the US.

      - Comply with the Manufacturer’s requirements as necessary to provide the specified warranty.

    - PRODUCT QUALITY ASSURANCE PROGRAM: Manufacturer shall be an ISO 9001 registered company.

    - ACCEPTABLE MANUFACTURER:

      - PERFORMANCE ROOF SYSTEM, INC., A SOPREMA GROUP COMPANY, located at: 4800 Dr. Martin Luther King Jr. Blvd., Kansas City, MO  64130; Tel: 816-921-0221; Tel 800-727-9872; Website: www.performanceroofsystems.us

      - Acceptable Alternate Manufacturers:  _________________________

  - ROOFING SYSTEM

    - ROOFING SYSTEM BASIS OF DESIGN: PERFORMANCE ROOF SYSTEM, INC., A SOPREMA GROUP COMPANY

  - THERMAL INSULATION SYSTEM

    - THERMAL BARRIER

      - GYPSUM ROOF BOARD

        - National Gypsum Company, DEXcell Glass Mat Roof Board, DEXcell FA Glass Mat Roof Board:

          - Gypsum core, glass fiber-faced, roof board:

          - Thickness: 5/8 in (1/2 in)

          - Dimensions: 4 x 4 foot or 4 x 8 foot boards

          - Facer:  Glass fiber.

          - Meets or exceeds ASTM C1177/C1177M.

        - Georgia Pacific Gypsum LLC, DensDeck Roof Board, DensDeck Prime Roof Board: Gypsum core, glass fiber-faced, roof board:

          - Thickness: 5/8 in (1/2 in)

          - Dimensions: 4 x 4 foot or 4 x 8 foot boards

          - Facer:  Glass fiber.

          - Meets or exceeds ASTM C1177/C1177M.

      - CEMENT ROOF BOARD

        - National Gypsum Company, DEXcell Cement Roof Board

          - Portland cement, lightweight aggregate and glass fiber mesh roof board.

          - Thickness: 7/16 in.

          - Dimensions: 4 x 4 foot or 4 x 8 foot boards

          - Facer: None

          - Meets or exceeds ASTM C1325.

        - United States Gypsum, Securock Brand Cement Roof Board:

          - Portland cement, lightweight aggregate and glass fiber mesh roof board.

          - Thickness: 1/2 in.

          - Dimensions: 4 x 4 foot or 4 x 8 foot boards

          - Facer: None

          - Meets or exceeds ASTM C1325.

    - RIGID INSULATION

      - POLYISOCYANURATE INSULATION:

        - DERBIBOARD: Closed cell polyisocyanurate foam core bonded on each side to a glass fiber-reinforced felt facer.

          - Thickness: 0.0 in minimum board thickness. Total thickness to meet specified insulation system thermal resistance ‘R’ value

          - Dimensions: 4 x 4 ft or 4 x 8 ft boards

          - Meets or exceeds ASTM C1289, Type II, Class 1, Grade 2 (20 psi). Grade 3 (25 psi).

        - DERBIBOARD Tapered:  Closed cell polyisocyanurate foam core bonded on each side to a glass fiber-reinforced felt facer, tapered to provide slope.

          - Taper:  1/8, ¼, 1/2 in per foot.  Insulation, crickets and saddles provided with taper as required for positive roof slope.

          - Dimensions: 4 x 4 ft boards

          - Meets or exceeds ASTM C1289, Type II, Class 1, Grade 2 (20 psi). Grade 3 (25 psi).

        - DERBIBOARD CA:  Closed cell polyisocyanurate foam core bonded on each side to a coated inorganic glass-reinforced facer.

          - Thickness: 0.0 in minimum board thickness. Total thickness to meet specified insulation system thermal resistance ‘R’ value.

          - Dimensions: 4 x 4 ft or 4 x 8 ft boards

          - Meets or exceeds ASTM C1289, Type II, Class 2, Grade 2 (20 psi). Grade 3 (25 psi).

          - Meets or exceeds ASTM D3273 for resistance to mold growth.

        - DERBIBOARD CA Tapered:  Closed cell polyisocyanurate foam core bonded on each side to a coated inorganic glass-reinforced facer, tapered to provide slope.

          - Taper:  1/8, ¼, 1/2 in per foot.  Insulation, crickets and saddles provided with taper as required for positive roof slope.

          - Dimensions: 4 x 4 ft boards

          - Meets or exceeds ASTM C1289, Type II, Class 2, Grade 2 (20 psi). Grade 3 (25 psi).

          - Meets or exceeds ASTM D3273 for resistance to mold growth.

      - MINERAL WOOL INSULATION:

        - SOPREMA SOPRAROCK DD, Roxul TopRock DD: Rigid, dual-density mineral wool insulation board.

          - Dimensions: 4x4 ft

          - Thickness:  2 to 6 in maximum, in ½ in increments, flat board stock only.

          - Total thickness to meet specified insulation system thermal resistance ‘R’ value.

          - Meets or exceeds ASTM C726.

        - SOPREMA SOPRAROCK DD PLUS (Roxul TopRock DD Plus): Rigid, dual-density mineral wool insulation board with sanded bitumen surfacing.

          - Dimensions: 4x4 ft

          - Thickness:  2 to 6 in maximum, in ½ in increments, flat board stock only.

          - Total thickness to meet specified insulation system thermal resistance ‘R’ value.

          - Meets or exceeds ASTM C726.

    - COVER-BOARD

      - ASPHALTIC ROOF BOARD

        - SOPREMA  SOPRABOARD: Mineral fortified, asphaltic roof substrate board with glass fiber facers.  For use as roof cover-board and for vertical flashing substrate.  ASPHALTIC ROOF BOARD shall be manufactured by the membrane supplier.

          - Thickness:  1/8 in  1/4 in

          - Dimensions: 4 x 4 ft, 4 x 5 ft and 4 x 8 ft acceptable for mechanical attachment, insulation adhesive or asphalt application.

          - Water absorption: Less than 1 percent per ASTM D994.

          - Impact resistance:  Included in FM Approvals per 4450/4470 for FM Severe Hail (SH) rating.

          - Compressive strength, psi (kPa) measured at 50 percent compression, per ASTM C472:

            - 1/8 in board:  1,610 (11,100)

            - ¼ in board: 1,320 (9,100)

          - Puncture resistance,  lbf (N) per ASTM E154:

            - 1/8 in board:  90 (400)

            - ¼ in board: 100 (445)

      - GYPSUM ROOF BOARD

        - National Gypsum Company, DEXcell FA Glass Mat Roof Board:

          - Gypsum core, glass fiber-faced, roof board:

          - Thickness: 5/8 in 1/2 in 1/4 in

          - Dimensions: 4 x 4 ft or 4 x 8 ft boards

          - Facer:  Glass fiber.

          - Meets or exceeds ASTM C1177/C1177M.

        - Georgia Pacific Gypsum LLC, DensDeck Prime Roof Board: Gypsum core, glass fiber-faced, factory primed, roof Cover-board.

          - Thickness:  5/8 in  1/2 in  1/4 in

          - Dimensions:  4 x 4 ft or 4 x 8 ft boards.

          - Facer:  Factory primed, glass fiber.

          - Meets or exceeds ASTM C1177/C1177M.

      - CEMENT ROOF BOARD

        - National Gypsum Company, DEXcell Cement Roof Board

          - Portland cement, lightweight aggregate and glass fiber mesh roof board.

          - Thickness: 7/16 in.

          - Dimensions: 4 x 4 ft or 4 x 8 ft boards

          - Facer: None

          - Meets or exceeds ASTM C1325.

        - United States Gypsum, Securock Cement Roof Board

          - Portland cement, lightweight aggregate and glass fiber mesh roof board.

          - Thickness: 7/16 in.

          - Dimensions: 4 x 4 ft or 4 x 8 ft boards

          - Facer: None

          - Meets or exceeds ASTM C1325.

      - HIGH DENSITY POLYISOCYANURATE COVER-BOARD

        - Hunter H-Shield HD (Atlas ACFoam-HD Cover-Board) :  ½ in thick, high density polyisocyanurate foam core bonded on each side to a coated inorganic glass-reinforced facer.

          - R 2.5 for ½ in thickness.

          - Dimensions: 4 x 4 ft or 4 x 8 ft boards

          - Meets or exceeds ASTM C1289, Type II, Class 4, 100 psi.

          - Meets or exceeds ASTM D3273 for resistance to mold growth.

    - INSULATION CANT AND TAPERED STRIP

      - CANT STRIP, APP MODIFIED BITUMEN

        - DERBICANT CANT STRIPS: APP Modified bitumen cant strips.

          - Length: 39 ¾” sections.

          - Cross-section dimensions:  1.25” thick x 2” in face width.  2.25” in thick x 3.25” in face width.  Size as required for flashing conditions.

          - Surface:  APP Modified Bitumen

      - CANT STRIP, EXPANDED PERLITE

        - High density, laminated board made of high strength fibers and expanded perlite.

          - Length: 4 ft sections.

          - Cross Section dimensions: 1 in thick x 3 in face, 1 in thick x

          - 4 in face, 1.5 in thick  x 4 in face, 1.5 in thick  x 5 in face. Size as required for flashing conditions.

          - Meets or exceeds ASTM C728.

      - TAPERED EDGE STRIP AND BOARDS:

        - Expanded perlite, blended with binders and fibers.

          - Dimensions:  6 in x 1/2 in, 12 in x 1/2 in, 1 in or 1-1/2 in, 18 in x 1 in or 1-1/2 in.  Size as required.

          - Meets or exceeds ASTM C728.

    - INSULATION ADHESIVE

      - POLYURETHANE FOAM INSULATION ADHESIVE

        - SOPREMA DUOTACK 365:   Two-component, polyurethane foam insulation adhesive, applied in ribbons from cartridges or two-component bulk packaging with pump-driven delivery system.

          - Ribbon size:  1/2 in to 3/4 in wide.

          - Ribbon spacing:  As required to meet specified wind uplift resistance performance.

            - Field of Roof (Zone 1): 	12 in on-centers

            - Perimeter of Roof (Zone 2): 	6 in on-centers

            - Corners of Roof (Zone 3): 	4 in on-centers

        - SOPREMA DUOTACK SPF:  Two-component, polyurethane foam insulation adhesive, applied in ribbons from a dual canister-based delivery system.

          - Ribbon size:  2-1/2”

          - Ribbon spacing: As required to meet specified wind uplift resistance performance.

            - Field of Roof (Zone 1): 	12 in on-centers

            - Perimeter of Roof (Zone 2): 	6 in on-centers

            - Corners of Roof (Zone 3): 	4 in on-centers

      - ASPHALT INSULATION ADHESIVE

        - MOPPING ASPHALT:  Approved for use as insulation adhesive, complying with ASTM D312, Type III or IV.   The Equiviscous Temperature (EVT), the finished blowing temperature (FBT) and the flash point (FP) shall be indicated on each container.

            - Application Rate:  Full coverage, applied at EVT for a nominal rate of 23-25 lbs/square.

  - ACCESSORIES

    - PRIMERS:

      - ASPHALT ROOF PRIMER:  Asphalt cut-back primer.  Primer for the preparation of membrane substrates for asphalt, heat-welded, hot asphalt and COLPLY ADHESIVE, solvent-based, cold adhesive-applied and cement applications.

        - Meets or exceeds ASTM D41

        - VOC content:  348 g/L

      - DERBIBASE SA PRIMER: 0 g/L VOC solvent, self-adhesive membrane primer.  Low VOC, solvent-based primer for the preparation of membrane substrates for self-adhered APP membrane and self-adhesive APP flashing applications.

    - MOPPING ASPHALT

      - MOPPING ASPHALT pre-approved in writing by membrane manufacturer for use for applying the specified insulation.

        - Application Rate:  Solid mopping, full coverage at 23-25 lb per square and as required for specified approvals.

        - Application Temperature:  Apply asphalt at the published EVT and no less than 400(F (204(C) at the point of contact when applying the SBS-modified bitumen membrane into the asphalt.

        - The Equiviscous Temperature (EVT), the finished blowing temperature (FBT) and the flash point (FP) shall be indicated on each container.

        - Meets or exceeds ASTM D312, Type IV as listed in Table I.

    - INSULATION FASTENERS AND PLATES

      - PERLOK #12 DP Drill Point Roofing Fasteners, Phillips Truss Head:  Membrane base ply and insulation fastener.

      - PERLOK #12 DPH Drill Point Roofing Fasteners, Hex Head:  Membrane base ply and insulation fastener.

      - PERLOK #12 PA and PAH Pre-Assembled Screws & Plates:  Pre-assembled membrane base ply and insulation fastener.

      - PERLOK #14HD Drill Point Roofing Fasteners, Phillips Truss Head:  Membrane base ply and insulation fastener.

      - PERLOK #14HDB-SS Stainless Steel Heavy Duty Bi-Metal, Phillips Truss Head:  Membrane base ply and insulation fastener.

      - PERLOK #15EHD Drill Point Roofing Fasteners, Phillips Truss Head:  Membrane base ply and insulation fastener.

      - PERLOK PFC Purlin Fastener: Membrane base ply and insulation fastener for standing seam metal recover applications.

      - PERLOK ¼” Concrete Spike: Membrane base ply and insulation fastener over structural concrete decking.

      - PERLOK Fluted Nail Concrete Fastener: Membrane base ply and insulation fastener over structural concrete decking.

      - PERLOK TL Lightweight Fasteners & Plates: Membrane base ply and insulation fastener over gypsum and tectum roof decks.

      - PERLOK VERSA FAST FASTENERS and 3 in VERSA FAST PLATE:  Membrane base ply fastener and seam plate assembly.  Inlcudes options for multiple fasteners per 3 in plate.

- EXECUTION

  - EXAMINATION

    - Examination includes visual observations, qualitative analysis, and quantitative testing measures as necessary to ensure conditions remain satisfactory throughout the project.

    - Conduct qualitative insulation adhesive adhesion tests, or quantitative bonded pull tests as necessary to ensure satisfactory adhesion is achieved.

    - The contractor shall examine all roofing substrates including, but not limited to: insulation materials, roof decks, walls, curbs, rooftop equipment, fixtures, and wood blocking.

    - The applicator shall not begin installation until conditions have been properly examined and determined to be clean, dry and, otherwise satisfactory to receive specified roofing materials.

    - During the application of specified materials, the applicator shall continue to examine all project conditions to ensure conditions remain satisfactory to complete the specified roofing system.

  - PREPARATION

    - Before commencing work each day, the contractor shall prepare all roofing substrates to ensure conditions are satisfactory to proceed with the installation of specified roofing materials.  Preparation of substrates includes, but is not limited to, substrate repairs, securement of substrates, eliminating all incompatible materials, and cleaning.

    - Where conditions are found to be unsatisfactory, work shall not begin until conditions are made satisfactory to begin work. Commencing of work shall indicate contractor’s acceptance of conditions.

  - PRIMER APPLICATION

    - Apply the appropriate specified primer to dry, compatible substrates as required to enhance adhesion of new specified roofing materials.

    - Apply primer using brush, roller, or sprayer at the rate published on the product data sheet.

    - Asphalt Primer:  Apply ( ASPHALT ROOF PRIMER) primer to dry compatible masonry, metal, wood and other required substrates before applying asphalt.

    - Self-Adhesive Membrane Primer: Apply (DERBIBASE SA PRIMER) to dry, compatible substrates as required to enhance adhesion of self-adhesive membrane plies.  Ensure self-adhered membrane primer is tacky to-the-touch, but not wet.  Primer should not transfer to the finger tips when touched.

    - Project conditions vary throughout the day.  Monitor changing conditions, monitor the drying time of primers, and monitor the adhesion of the membrane plies.  Adjust primer and membrane application methods as necessary to achieve the desired results.

  - INSULATION FASTENER APPLICATION

    - Fasten (Thermal Barrier, Insulation Base Layer, Insulation, Cover-board) to the deck using specified insulation fasteners and plates.

    - Evenly distribute fasteners as required by the board manufacturer’s published requirements.

    - Fasten the insulation to meet the specified wind uplift resistance performance requirements and warranty requirements.

    - Minimum insulation fastening requirement:

      - Field of Roof (Zone 1): 		1 fastener per 0.00 square ft

      - Perimeter of Roof (Zone 2): 		1 fastener per 0.00 square ft

      - Corners of Roof (Zone 3): 		1 fastener per 0.00 square ft

    - Minimum insulation fastening requirement:

      - Field of Roof (Zone 1): 		00 fasteners per 4x8 ft board.

      - Perimeter of Roof (Zone 2): 		00 fasteners per 4x8 ft board.

      - Corners of Roof (Zone 3): 		00 fasteners per 4x8 ft board.

    - For insulation and Cover-boards located partially within the defined perimeter and/or corners, install fastening for the entire board as specified herein.

  - INSULATION ADHESIVE APPLICATION

    - Apply the specified two-component insulation adhesive to adhere (Insulation Base Layer, Insulation Layers, Cover-board) to the deck and insulation substrate(s).

    - Follow insulation adhesive product data sheets and published general requirements for installation requirements.

    - Apply insulation adhesive in uniform ribbons, 1/2 in to 3/4 in wide.

    - Immediately install insulation components into insulation adhesive, and apply weight to ensure the materials maintain full contact with all ribbons for complete adhesion.  Do not allow insulation adhesive to skin-over before placing the insulation materials into the adhesive.

    - Adhere the insulation system to meet the specified wind uplift resistance performance and specified warranty requirements.

    - Minimum insulation adhesive ribbon spacing:

      - Field of Roof (Zone 1): 12 in on-centers.

      - Perimeter of Roof (Zone 2): 6 in on-centers.

      - Corners of Roof (Zone 3):  4 in on-centers.

  - MOPPING ASPHALT APPLICATION

    - Fully adhere (Insulation Base Layer, Insulation Layers, Cover-board) to deck and insulation substrate(s) using specified mopping asphalt.

      - Mopping asphalt manufacturer and type shall be preapproved by the manufacturer.

      - Refer to mopping asphalt supplier published values for Softening Point, Minimum Flash Point (FP), Finished Blowing Temperature (FBT) and Equiviscous Temperature (EVT).

      - To avoid risk of fire do not heat asphalt at or above the Flash Point temperature.

      - The EVT is the temperature at which the mopping asphalt viscosity is 125 centistokes.

      - Apply mopping asphalt within +/- 25(F (14(C) of the published EVT to obtain the nominal 23 to 25 pounds per square coverage rate.

      - Refer to the EVT provided by the asphalt supplier.  Typically, the Type III asphalt application temperature should be within 365 to 435(F (185 to 224(C) and Type IV asphalt application temperature should be within 400 to 475(F (204 to 246(C) at the point of application when installing roofing materials into the hot asphalt.

      - The contractor shall monitor asphalt application temperature, and shall record the temperature during application.

    - Install full coverage of mopping asphalt applied at 25-30 lbs/square, and as required to meet specified wind uplift approvals and warranty requirements.

    - Immediately install insulation components into hot asphalt, and apply weight to ensure the insulation materials maintain full contact with the asphalt for full adhesion.

  - INSULATION SYSTEM APPLICATION

    - Follow insulation system component product data sheets, published general requirements and, approvals.

    - Install all insulation system components on clean, dry, uniform and, properly prepared substrates.

    - All insulation system boards shall be carefully installed and fitted against adjoining sheets to form tight joints.

    - Insulation system boards that must be cut to fit shall be saw-cut or knife-cut in a straight line, not broken. Chalk lines shall be used to cut insulation components. Uneven or broken edges shall not be accepted. Remove dust and debris that develops during cutting operations.

    - Stagger successive layers of insulation 12 in vertically and laterally to ensure board joints do not coincide with joints from the layers above and below.

    - Crickets, saddles, and tapered edge strips shall be installed before installing Cover-boards.

    - Install tapered insulation, saddles and crickets as required to ensure positive slope for complete roof drainage.

    - Cover-boards shall be installed to fit tight against adjacent boards.  When required by the Cover-board manufacturer, a uniform gap shall be provided between Cover-boards using a uniform guide placed between board joints to form a gap between all boards during installation.

    - The finished insulation system surface shall be tight to, and flush with, adjacent substrates to form a satisfactory substrate to install specified roof membrane and flashings.

    - Install specified cants where required for membrane flashing transitions.

  - CLEAN-UP

    - Clean-up and properly dispose of waste and debris resulting from these operations each day as required to prevent damages and disruptions to operations.

END OF SECTION